"Nanocomposites and nanomaterials"

Structure, optical properties and photocatalytic activity of undoped, La2O3-doped ZnO nanocomposites
Chudinovych O. V.1,2, Myroniuk D. V.1, Myroniuk L. A.1, Danylenko I. M.3, Olifan O. I.1
1 Frantsevich Institute for Problems of Materials Science of the NAS of Ukraine,
Krzhyzhanovsky Str., 3, Kyiv-03142, Ukraine.
E-mail: chudinovych_olia@ukr.net
2 National Technical University of Ukraine “Igor Sikorsky Kyiv Polytechnic Institute”, Peremohy Av., 37, Kyiv-03056, Ukraine.
3 Lashkaryov Institute of Semiconductor Physics of the NAS of Ukraine,
Nauky Av., 41 Kyiv-03039, Ukraine.

Zinc oxide is an important material due to its optical, photocatalytic, and magnetic properties. ZnO can be an effective photocatalytic nanomaterial due to the high generation rate and distribution of photoinduced electrons e and holes h+. Doping ZnO with rare earth elements has a great influence on the photocatalytic efficiency of ZnO [1].
The undoped and La2O3-doped ZnO nanoparticles were synthesized using a chemical method from Zn2+ and La3+ nitrates solutions. Investigate the X-ray diffraction patterns of undoped and La2O3-doped ZnO nanoparticles on a “Dron-3M” X-ray diffractometer. The undoped ZnO nanoparticles are identified as a wurtzite structure ZnO. The XRD patterns of the La2O3-doped ZnO do not show any other peaks corresponding to La, La2O3 or any other additional phases associated with impurities. These indicate the ideal solubility and homogeneity of La3+ ions in the ZnO lattice.
Micro-Raman scattering measurements were carried out to study the influence of La3+ doping on the structural and vibrational properties of ZnO samples.

This work supported by the research project of the NAS of Ukraine “Creation of promising materials based on ZnO doped REE for use in catalysis”.

Yu Y., Chen G., Zhou Y., Han Z. Recent advances in rare-earth elements modification of inorganic semiconductor-based photocatalysts for efficient solar energy conversion: A review // J. Rare Earths. - 2015. - V. 33(5). - P. 453-462.